지르코니아 담지 니켈촉매상에서 메탄의 이산화탄소 개질반응

이신생, 장종산, 박상언

한국화학연구소 공업촉매팀

# Carbon Dioxide Reforming of Methane over Zirconia-Supported Ni Catalysts

Xinsheng Li, Jong-San Chang, Sang-Eon Park*

Industrial Catalysis Research Team, Korea Research Institute of Chemical Technology (KRICT), Daeduck Science Town, P.O.Box 107, Taejon, Korea 305-606

INTRODUCTION

- Great attention is being paid to the conversions of methane and carbon dioxide, respectively, because CH4 is the main component in natural gas, and CO2 concerns global warming problem. So that study on catalytic conversion of CO2 or CH4 becomes an attractive and challenging subject. One of the best solutions for both of them is CO2 reforming of CH41,2. There are two series of catalysts studied towards this direction, i.e., noble metal and cheap metal catalysts. In the point of view of economic cost, the best representative of cheap metals, namely nickel based catalyst presents the most promise application in this direction. Though the conventional nickel supported on alumina catalyst has high activity to the reforming reaction, there is a serious problem of catalytic deactivation mainly caused by coke formation. The key point in developing one new type of nickel based catalyst for dry reforming is searching for a suitable support2-4. Zirconia acted as catalyst support is being widely tested by catalytic reaction because of its unique chemical properties. In the present study, we report some features of dry reforming reaction on Ni/ZrO2, among which nickel loading covers a wide range. The middle nickel loading catalyst had the highest activity for methane and carbon dioxide conversion. Different promoters were introduced to Ni/ZrO2 catalysts and showed different promotion to the reaction.

EXPERIMENTAL

1. Catalyst

All  the nickel catalysts were prepared by impregnation of supports with solution of nickel nitrate, drying at 100C overnight, and calcination at 500C for 4h. After it was calcined at 900C for 8h, zirconia (Extra Pure, Hayashi Pure Chemical Industries, Ltd.) was used to prepare the Ni/ZrO2 catalysts varying nickel loading  from 2.5wt% to 23wt%. One home-made zirconia (marked as ZrO2-H) and four modified zirconia were prepared by sol-gel method. Briefly the procedure is described as introducing solution of zirconyl chloride or mixture of zirconyl chloride and the corresponding foreign metal salt to ammonia solution under strongly stirring, the precipitate was filtered and washed, dried at 100C overnight and calcined at 900C for 8h.  The atomic ratio of zirconium to promoter is 5:1.

2. Activity Tests

Activity tests were carried out in a quartz reactor, which was protected by a stainless steel tube for a safe purpose.  Besides one thermal couple controlled the oven temperature, another thermal couple was inserted into the reactor and directly contacted the catalyst bed. 50mg catalyst, mixed with 250mg quartz sand, was used. The flow rate of the reactant gases CH4:CO2:N2=1:1:3 is 50ml/min. Prior to reaction test, the catalyst was reduced in 5%H2-N2 (in vol.) at 700C for 2h, and then purged with N2 for 10min, and then decrease temperature to 500C. The reaction was carried out at 500, 600, 700, 750, 800,and 850C respectively. The products were on line analyzed, using nitrogen as an internal reference gas, on a thermal conductivity detector of Chrompack CP9001 equiped with a PLOT Fused Silica capillary column.

3. Characterization

The specific surface areas of supports were measured on a Micromeritics’ sorption analyzer (model ASAP 2400) after degas at 300C . Powder X-ray diffraction (XRD) were measured on a Rigaku diffractometer with a Ni-filtered Cu-Ka (alpha) radiation. Thermogravimetric analysis (TG) was performed on an Intelligent Gravimetric Analyser. The sample was pre-reduced at 700C for 2h,  purged with helium for 20min, and then cooled down to room temperature in helium. Afterwards, temperature programmed surface reaction was performed in 50%CH4-50%CO2 at a flow rate of 20ml/min and a heating rate of 10C/min.

RESULTS AND DISCUSSION

1. The importance of internal temperature control

Because CO2 and CH4 reforming reaction is endothermic, temperature difference between oven and the catalyst bed is caused by not only temperature gradient but also the reaction itself.  As seen in Table 1, the temperature change caused by reaction becomes large when the catalyst was increased to high temperature. So that, it is necessary to have an internal temperature indicator, therefor the reaction temperature can be adjusted to the setting point.

Table 1   Temperature change of catalyst bed of Ni/ZrO2 catalyst

Oven temp. (C) a		517	 616	719	770	819	866

Reaction Temp. (C)b	500	 600	700	750	800	850

Temp. without Reaction (C)c	501	 603	707	759	809	859

a Temperature of oven. b Temperature of catalyst bed with reactant gases CH4:CO2:N2=1:1:3.

c Temperature of catalyst bed with N2 flow by switching off the valves of CH4 and CO2.

2. Blank Test

The support zirconia was tested during 500-900C as blank experiment.  When reaction temperature is below 750C, there is no detection of H2 and CO production. During reaction temperature range 750-850C, there were traces of hydrogen and carbon monoxide detected, for example Y(H2)= 0.0011and Y(CO)=0.0011 at reaction temperature TR=850C.

Hydrogen and carbon monoxide behave differently on the support zirconia. It was seen that CO2 conversion occurred even at 500C, and changed slightly during the temperature range 500-750C, and then increased as increasing reaction temperature. In contrast, CH4 shows no activity on zirconia during 500-700C, When temperature increased to above 750C, there is a trace of methane to decomposition giving rise to hydrogen. In the activity measurement of Ni-containing catalysts, the relative error caused by zirconia support and the reactor is calculated to be less than 5% for CO2, and 1% for CH4, H2 and CO, respectively, in the present study.

3. Ni/ZrO2 Catalysts

We have studied the effects of nickel loading and reaction temperature on CH4 and CO2 conversions, respectively.  It is observed that both CH4 and CO2 conversions increased with a rise of reaction temperature. Among the catalysts with variance of Ni loading from 2.5% to 23%, 8.50% and 13.21% Ni/ZrO2 catalysts exhibited the highest activity of the reforming reaction.

The lifetime was tested using 13.21%Ni/ZrO2 catalyst at 850C and 750C, respectively, as displayed in Fig. 1. It is seen that CH4 and CO2 conversions nearly remained at the same level when the reaction was carried out at 850C for 20h. Similarly in the case of 750C, CH4 and CO2 conversions changed slightly after 30h reaction. However, high temperature test makes some negative effect on the activity as depicted in Fig.2. On all the Ni/ZrO2 catalysts, the activities for CH4 and CO2 conversions at 750C for the catalysts before 850C test (marked as -BE-850C) are higher than that of the catalysts after 850C test (marked as -AF-850C).

TG measurement of coke formation on reduced 22.61Ni/ZrO2 catalyst shows that coke formation started at about 450C, and reached 98.5% when temperature increased to about 660C. When the temperature was kept at 700C for 6h, the weight continually increased by 1.5%. This indicates that most of the coke was formed at temperatures below 700C during CO2 reforming of CH4 over Ni/ZrO2 catalyst.

4. Promoted Ni/ZrO2 Catalysts

The promotion of adding La, Mg, Ce and Mn to Ni/ZrO2 is studied in the reaction temperature range 500-850C, herein one Ni/ZrO2 catalyst using home-made zirconia (marked as -H) was also tested as reference.  Besides the general trend of that activities increased with increasing temperature, the La and Mg promoted Ni/ZrO2 catalysts exhibit higher conversions of CH4 and CO2 than that of the un-promoted catalyst, whereas the Ce and Mn promoted catalysts show lower activity than that of the reference sample in the temperature range 600-850C. Their activity is in the order: Ni/Zr0.87La0.13O2 > Ni/Zr0.87Mg0.13O2 > Ni/ZrO2> Ni/Zr0.87Ce0.13O2 > Ni/Zr0.87Mn0.13O2.

From XRD measurement, it was seen that there is only a tetragonal phase of zirconia formed on Zr0.87La0.13O2 and Zr0.87Ce0.13O2 , a mixture of tetragonal phase and monoclinic phase appeared on Zr0.87Mg0.13O2 and ZrO2-H, and a monoclinic phase appeared on Zr0.87Mn0.13O2. In particular, a phase transformation from tetragonal phase to monoclinic phase occurs on Zr0.87Mg0.13O2 and ZrO2-H when Ni was introduced to the supports. However there is no such phase transformation observed on Ni/Zr0.87La0.13O2 and Ni/Zr0.87Ce0.13O2. These XRD data provide obvious evidence that the crystalline of zirconia does not take any key role in the catalytic behavior of these promoted Ni/ZrO2 catalysts.

TG measurement of coke formation on reduced 13.21Ni/ Zr0.87La0.13O2 catalyst showed different behavior from those phenomena observed on Ni/ ZrO2 catalyst. Coke formation on reduced Ni/ Zr0.87La0.13O2  started at 480C, and did not reach a steady state even when reaction was held at 700C for 1h. This result once again proves that Ni/ Zr0.87La0.13O2 is more active than Ni/ ZrO2 catalyst.

According to the “bi-functional” mechanism proposed by Mirodatos et al.5, the high activity caused by La and Mg promoters can be explained by that the La and Mg provide adsorbed site for CO2 to form surface carbonates and react with nickel-adsorbing carbon2, so that the Ni particle can be restored to their original state.

REFERENCES

1. Rostrup-Nielson, J.R.and Bak Hansen, J-H. :  J. Catal., 144, 38 (1993).

2. Chang, J-S., Park S-E. and Chon H.: Applied Catalysis A General, 145 , 111 (1996).

3. Bitter, J.H., Seshan K. and Lercher J.A.: J.Catal. : 171, 279 (1997).

4. Lercher, J. A., Bitter, J.H., Hally, W., Niessen, W. and Seshan, K.: (Eds. Hightower, J.W., Delgass, N., Iglesia, E. and Bell A.T.) 11th International Congress on Catalysis -40th Anniversary, Studies in Surface Science and Catalysis, Vol.101, p. 463.

5. Slagtrn A., Schuurman Y., Ceclercq C., Verykios X., and Mirodatos C. : J. Catal., 172, 118 (1997).

Fig.1  Changes in CH4 and CO2 conversions at 750C and 850C versus

reaction time on 13.21%Ni/ZrO2 catalyst.

Fig.2  Comparison of CH4 and CO2 conversions at 750C for Ni/ZrO2 catalysts

before and after 850C test.