리포솜 피부외용제에 함유된 초산 하이드로코르티손의 안정성

배수경, 김진철, 김종득

한국과학기술원 화학공학과

Stability of Liposomally Entrapped Hydrocortisone Acetate Contained in Different Dermatological Bases

Soo Kyoung Bae, Jin-Chul Kim, and Jong-Duk Kim

Dept. of Chem. Eng., Korea Advanced Institute of Science and Technology

Introduction

Even though liposomes are known to have potential to be used as a topical drug carrier (1,2), their stability in long term storage is a crucial problem in developing liposomal dermatological bases. In addition, when the drug to be entrapped is hydrophobic and degradable in aqueous media, its stability problem may discourage the attempts to apply the liposomal system in preparing topical applications.

In this work, hydrocortisone acetate (HCA), an anti-inflammatory agent degradable in water(3), was tested for its stability in the liposomal system. Three commonly applied dermatological semi-solid bases, namely Hydrogel, Cream, and Poly(ethylene glycol)(PEG)  hydrophilic ointment, were prepared to contain liposome-encapsulated HCA. Then, the effects of liposome entrapment, types of bases, base viscosity, and lipid purity on the drug stability were investigated.

Methods

Liposomes were produced by the precipitation method in which ethanol was evaporated from the mixture of purified water and ethanol with lipids and HCA dissolved in it. Hydrogel was prepared by swelling carboxymethylcellulose with propylene glycol and egg PC liposome suspension. Another batch of Hydrogel was prepared to contain the same quantities of the same ingredients, except free-form HCA instead of liposomal HCA. Cream was prepared by melting stearyl alcohol, mineral oil, and surfactants together and emulsifying with liposomal suspension. PEG hydrophilic ointment was prepared by mixing melted poly(ethylene glycol) of different molecular weights and white petrolatum with liposomal suspension. Cream and PEG ointment samples were prepared in two sets each, one set with egg PC(60% purity) liposomes and the other with soybean PC(90% purity) liposomes. Water contents in the three formulations were 84 wt.% in Hydrogel, 34 wt.% in Cream, and 14 wt.% in PEG ointment. All the samples were all stored at room temperature, 30°C, and 40°C for 4 weeks. During the storage period, each of the different samples from each storage temperature was taken for the drug stability test by HPLC at a one-week interval.

A JASCO HPLC pumping set with JASCO UV detector was used in the quantitative analysis of HCA. The wavelength for the absorbance was 214 nm, and the pumping flow rate was 1.5 ml/min. The mobile phase was a mixture of deionized water, methanol, and acetonitrile in the ratio of 5:2:3. The separation column used in this experiment was a C18 column with 10-mm particles.

The base viscosity was measured with Haake Rotovisco® RV 20. Approximately 6ml of a base sample was placed in between two cylinders, one of which rotated to exert torque onto the sample, and shear viscosity was obtained. The viscosity data were obtained at room temperature, 30°C, and 40°C for each base sample.

results and discussion

Three comparisons were made to analyze the effects of liposome encapsulation, base materials, and lipid purity on the stability of HCA. First, the stabilities of liposomal HCA and free-form HCA contained in the Hydrogel bases, both having the same water contents, were compared, and liposomal HCA was found to be more stable than free HCA(See Figure 1). It is obvious that liposomes have influenced on the drug stability in a protective manner. The HCA precipitate particles staying within the hydrophobic domain of the liposomal membranes may have a lower probability of getting in contact with water molecules dispersed in the base. Therefore, degradation reaction may occur in a less degree in the liposomal case than in the free-drug case.

Secondly, when the three bases were all prepared with HCA encapsulated in egg PC liposomes, the stability of HCA was maintained higher in Hydrogel than the other two bases, Cream and PEG ointment(See Figure 2). Since the Hydrogel base contained the largest percentage of water by weight, it was expected to result in the lowest drug stability. However, Hydrogel polymer chains might have caused reduction in the diffusivities of the drug particles and of the vesicles. The polymer chains form an extensive network, trapping the liposomes in the network and holding water molecules by hydrogen bonding. Therefore, liposomes may remain in an intact form and segregate HCA particles from water molecules. Therefore, the environment provided by Hydrogel was favorable for the physical stability of liposomes, extending influence onto the drug stability. In the case of Cream, the surfactant molecules added as emulsifiers are suspected to have penetrated into the liposomal membranes and have caused defects or breakage of the membranes. Then, the evenly dispersed water phase domains might have attacked the HCA particles in exposure. In the case of PEG ointment, the drug degradability was low compared to that in Cream because the water content in the former was low. However, the drug degradability was higher compared to that in Hydrogel as the lipid molecules dispersed in the PEG base might not be in proper assembly because of the low water content.

The base viscosities were compared as in Figure 3. The viscosity data of the bases indirectly indicate the degree of molecular diffusion within the bases. Greater energy consumption will be expected in diffusional movement in a highly viscous medium than in a less viscous medium. Hydrogel, which shows the highest viscosity among the three bases, has the highest drug stability. But, Cream and PEG ointment, having low viscosities, may allow more molecular movement to occur within the bases and provide more chances of molecular collision for reaction. The molecular movement effect may be also extended to the preservation of the liposomal assembly. Lipid molecules tend to go to thermodynamical equilibrium by molecular diffusion(4), and therefore liposomal bilayers are susceptible to breakage. But, the high viscosities of the semi-solid bases, especially that of Hydrogel, may prevent lipid molecules from breaking away from the bilayer arrangement, thereby maintaining the protective role for HCA particles.

Lastly, Cream and PEG ointment samples were prepared with egg PC(60% purity) liposomes and soybean PC (90% purity) liposomes in separate batches,  and the stability of HCA was better in the samples with liposomes made of high purity lipid than in those of low purity lipid(See Figure 4). The impurities associated in the 60% PC could be mainly proteins and non-amphiphilic. lipids. Those macromolecules may penetrate into the liposomal membranes and deform the overall vesicle structure. Thus, when surfactant

Figure 1						Figure  2

molecules attack the vesicles, as in Cream, the vesicles are relatively easily destroyed. Meanwhile, 90% PC could maintain the liposome structure nearly intact and could endure the attack of surfactant molecules to a certain extent. PEG ointment had no apparent

influence on the lipid type because liposomes could not stay intact in the PEG environment where water was insufficient.

CONCLUSION

The HPLC analysis results for the HCA concentrations in those three samples showed that HCA was stable as being entrapped in liposomes. The protective hydrophobic lipid bilayer prevented the contact between HCA and the aqueous phase. The HPLC results for the HCA concentrations in the control samples containing free HCA without liposomal encapsulation showed that the contact between the drug and water molecules was crucial in drug degradation. Since the stability of the drug reflects the stability of liposomes contained in dermatological bases, the liposomal stability was shown to be the best in Hydrogel among the three base samples. The drug concentrations in Hydrogel at all temperatures were maintained above 90% for 4 weeks.

Figure 3				        Figure 4

REFERENCES

1. Touitou, E., H.E. Junginger, N.D. Weiner, T.Nagai, and M.Mezei. "Liposomes as Carriers for Topical and Transdermal Delivery." Journal of Pharmaceutical Sciences. 83(1994), 1189-1203.

2. Hope, Michael J. and C. Neil Kitson. "Liposomes : A Perspective for Dermatologists." Dermatologic Clinics. 11(1993), 143-154.

3. Florey, Klaus. “Hydrocortisone." In Florey, K. (ed.) Analytical Profiles of Drug Substances, vol.12. Acadimic Press. New York. 1983.

4. Gruner, Sol M. “Materials Properties of Liposomal Bilayers.” In Ostro, Marc J. (ed.)           Liposomes : From Biophysics to Therapeutics. Marcel Dekker, Inc. New York. 1987.