- 고정층 흡착탑내에서 유기용제의 비등온 흡착거동

- 심왕근, 양우철, *양재호, 문 희

- 전남대학교 응용화학공학부

*전남대학교 화학공학과

- Non-Isothermal Adsorption Behavior of VOCs in Fixed-Bed Adsorber

- Wang Geun Shim, Woo Chul Yang, *Jai Ho Yang, Hee Moon

Faculty of Applied Chemical Engineering, Chonnam National University, Kwangju 500-757

*Department of Chemical Engineering, Chonnam National University, Kwangju 500-757

- Introduction

Solvent vapors have been used as dissolving and cleaning agents in many industrial processes such as printing, film coating, and manufacturing of magnetic tapes and electronic chips etc. The emission of solvent vapors from these industrial processes has not only caused severe air pollution but also great loss of valuable chemicals. One consequence of these manufacturing operations is that large amounts of organics are being emitted to the atmosphere each year. VOCs are among the most common pollutants emitted by chemical process industries. Accordingly, VOC emission control is a major portion of environmental activities. Therefore the proper recovery of volatile solvent vapors from industries has multiple purposes such as the reduction of production cost, energy saving, and the environmental protection.

Adsorption of Volatile Organic Compounds (VOCs) from air has been studied for a long time. The adsorption method would be an efficient and economic technique for recovering solvent vapors from their mixtures which contain 1000 ~ 3000 ppm of volatile solvents once a proper adsorbent can be found. In Korea, about 1000 tons of various solvents in a year have been used in many industrial processes as polyethylene coating and cleaning agents. The emissions from some industries contain BTX, MEK, and other valuable solvents which should be recovered to reduce production cost and air contamination.

The primary objectives of the present work are the recovery of a solvent vapor by a adsorption process and the theoretical analysis of adsorption bed dynamics based on a mathematical model. The present work is to obtain the pertinent adsorption and desorption data and to develop a mathematical model for the calculation of a non-isothermal adsorption process. Two major solvents, n-hexane, MEK which are mainly used in many industries are chosen and activated carbon was used as adsorbents for solvent recovery.

- Theoretical Model

The mathematical model of a non-isothermal, dynamic-column adsorption process basically requires transient material and energy balances. In this regard, both the adsorption equilibrium and kinetic aspects of the process must be accounted for. The model adopted here utilizes the Langmuir isotherm equation and a linear driving force (LDF) rate model to simplify the diffusional mass transfer inside adsorbnet particles. The LDF model is a lumped-parameter model for particle adsorption.

A simple model for a non-isothermal adsorption in a fixed bed is as follows;

- Mass balance:

-DL∂2C∂z2+v∂C∂z+∂C∂t+1−εερp∂q∂t=0

(1)

Heat balance, with axial thermal conduction:

(2)

(−ΔH)1−εε∂q∂t+2hεR(T−T0)=0−Kzε∂2T∂z2+vρgCg∂T∂z+ρgCg+1−εερgCs∂T∂t−

The mass-transfer rate inside particles can be represented by

∂q∂t=Ks(q∗−qs)

(3)

q∗qs=bCn1+bCnThe Langmuir  and Languir-Freundlich equation is used for adsorption equilibrium

(4)

q∗qs=bC1+bC

The PDEs representing the packed bed dynamics were solved by a numerical method called “method of lines (MOL)”. Eqs. 1-4 were first reduced to a set of ordinary differential equations (ODEs) by the method of lines. The resulting set of ODEs were integrated in terms of time using the subroutine DVODE of the International Mathematical and Statistical Library (IMSL).

- Experimental

The system in the present study was used for adsorbents (activated carbon) and n-hexane and MEK. Experimental adsorption and desorption runs were performed for various adsorbents. The operating conditions for all runs are as follows; T = 35oC and W (loading weight) = 3g. The apparatus was constructed with stainless steel tubes. It has three major sections: 1) preparation of vapors, 2) adsorption column in a water bath, and 3) analysis of gases. The gas flow line of nitrogen was divided into three branches, one is for pure nitrogen gas and the others are connected to solvent saturators. The concentrations of each solvent were evaluated from its saturated vapor pressure at a given temperature by assuming its vapor-liquid equilibrium state. All lines were sufficiently heated (more than water bath) to prevent the saturated solvent vapors from condensing in the steel tubes. The gas mixture of saturated solvent vapors and pure nitrogen gas was delivered to the adsorption section. The gas flow through the column was controlled by mass flow controllers with a read-out power supply which was precalibrated against a soap bubble flow meter covering a wide range of flow rates under experimental pressures. The gas mixture was heated to the experimental temperature in the preheating section before being charged to the fixed-bed adsorber. Two K-type thermocouples were installed at inlet and outlet sections of the packed column, and the temperatures were monitored continuously on a display recorder. The composition of exit gas stream from the adsorption section was determined using a gas chromatography, GC-14B model (Shimadzu), equipped with a hydrogen flame ionization detector. Helium was used as a carrier gas.

- Results and Discussions

The different models have been used to correlate experimental equilibrium data of n-hexane and MEK on activated carbon. Representative experimental data for n-hexane and MEK at three different temperatures, along with their Langmuir and Langmuir-Freundlich model fits, are shown in Fig. 1 and 2. For n-hexane and MEK, the Langmuir isotherm provides a less satisfactory fir compared to other isotherms. On the other hand, the Langmuir-Freundlich isotherm is perhaps superior, as it provides equally good fits over the entire concentration range. Fig. 3 and 4 show the temperature derivative plots for the   two isotherms, including experimental data (shown as points). The plots indicate that the Langmuir-Freundlich and Toth models similar gradient curves and correlate experimental temperature derivatives at both high and low concentrations reasonably well. The temperature derivative indicates the suitability of the isotherm model in simulating the shape and movement of the heat front in an adsorption process. Fig. 5 shows the effect of temperature on adsorption breakthrough curves for bed inlet temperatures of 35, 75, 175 and 275 oC. As the temperature decreases, more heat is generated and breakthrough curve is sharper during adsorption as we can see from the rise of temperature. Typical experimental adsorption breakthrough curves with the model simulation results are illustrated in Fig. 6. The isothermal model overpredicts the breakthrough time as one would expect. The breakthrough curve predicted from the adiabatic model exhibits the typical form. It is importatnt to note that the experimental breakthrough curve and breakthrough time are much closer to isothermal predictions than adiabatic predictions.

- References

1.  Farooq, S.; Ruthven, D.M. Ind. Eng.Chem.Res., 29, 1084 (1990)

2.  Hwang, K. S., Choi, D.K., Gong, S.Y., Cho, S.Y. Chem.Engng Sci. 52, 1111 (1997)

3.  Ruthven , D. M., “ Principles of Adsorption and Adsorption Process ”, Wiely, New York  (1984)

FFigure 1. Adsorption isotherms of n-hexane on AC

Figure 2. Adsorption isotherms of MEK on AC

Fig. 4. Temperature derivative of MEK  equilibrium isotherms.

FFig. 3. Temperature derivative of n-hexane  equilibrium isotherms.

FFig. 5. Effect of temperature on the concentration and temperature breakthrough curves.

FFig. 6. Typical adsorption breakthrough curves.