분무건조법에 의한 poly(N-isopropylacrylamide)

grafted ethylcellulose 입자의 열민감성에 관한 연구

±èº´À±, °Çü¼®, ±èÁ¾µæ

KAIST ÈÇÐ°øÇÐ°ú

Thermo-sensitive microparticles of poly(N-isopropylacrylamide)

grafted ethylcellulose by the spray drying method

Byoung-Yun Kim, Hyung-Seok Kang and Jong-Duk Kim

Department of Chemical Engineering, KAIST

INTRODUCTION

Recently keen attention has been paid to polymers which recognize and respond to external stimuli such as thermal energy, light, electricity, pH, ultrasound, and oscillating magnetic fields. To prepare external-stimuli-sensitive polymers, it is effective to utilize phase transition phenomena of polymers. Poly (N-isopropylacrylamide) (PNIPAM) is the most popular thermo-sensitive polymer due to its dramatic and reversible transition behaviors.

Spray drying method has been widely used for the preparation of microparticles due to the following advantages: It is a well-established technology, involves readily available equipment, and is able to produce large amounts of capsules. It is an expeditious, single-step process, and the resultant microparticles have a narrow size distribution.

The purpose of the present study is to prepare thermo-sensitive microparticles by the spray drying method. We synthesized graft copolymers of ethylcellulose (EC) as the hydrophobic component and poly (N-isopropylacrylamide) (PNIPAM) as the hydrophilic component to make thermo-sensitive material. Microparticles were prepared by the spray drying method. The drug used was allopurinol which is widely used in the treatment of hyperuricemia and chronic gout. The thermo-sensitive release behavior from this microcapsules was studied by conducting the release test at 25℃ (below the LCST) and 40℃ (above the LCST).

It can be expected that drug release from the thermo-sensitive microparticles will be applied to the site-specific drug delivery system by modulating the temperature of the target site.

EXPERIMENTAL

Synthesis and characterization of EC-g-PNIPAM

The polymerization process was carried out in chloroform/DMSO (50/50) ml solvent system. 2g of EC, various amounts (1, 2, 4, 8g) of NIPAM were dissolved in 100ml of chloroform/DMSO (50/50) ml solvent system under nitrogen bubbling for 1hr. Polymerization was initiated by 0.2g of APS and was carried out at 50℃ for 3h. After reaction, the polymerization mixture was poured onto excess amount of deionized water with vigorous magnetic stirring to precipitate the reaction product. The extraction of PNIPAM homopolymer was carried out by excess amount of deionized water for 1hr at room temperature for three times. After extraction the graft product was filtered, and vacuum dried. The composition of the graft copolymers were examined by Fourier Transform Infra Red Spectroscopy.

Preparation and characterization of microparticles

The microparticles were produced using B-191 mini spray-dryer. The experimental parameters of the process were set as follows: inlet temperature 40℃, outlet temperature 34-35℃, aspirator setting : 44-45mbar, pump setting : 7-8ml/min, spray-flow: 600NL/h. A 0.7mm nozzle was used throughout the experiments. 0.5g of allopurinol and 2.5g of polymer were dissolved in 100ml of dichloromethane to prepare microparticles. The ratio of drug to coating material was 1:5 and the total concentration of polymer and drug in the organic solution was 3%(w/w).

The size and morphology of the microparticles were characterized by scanning electron microscopy and particle size distribution was analyzed by Particle Counter Sys.

In vitro release rate experiments

Release tests of microparticles were carried out by dialysis membrane technique. 100mg of microcapsules were put into a dialysis membrane (MWCO: 12-14,000) filled with 7mL of PBS 7.4 solution containing 0.02% (w/v) Tween 80 (donor compartment). This membrane was put into 150mL of PBS 7.4 solution containing 0.02% (w/v) Tween 80 (acceptor compartment). The acceptor solution was stirred with a magnet bar at 100rpm. The temperature of the acceptor compartment was kept at 25℃ and 40℃ by a water bath respectively. The concentration of drug was measured by UV-Visible spectrophotometer at the wavelength of maximum absorbance (250 nm).

RESULTS AND DISCUSSION

Synthesis and characterization of EC-g-PNIPAM

As shown in figure 1 the grafting yield increases by increasing the concentration of NIPAM. The FTIR spectra of EC and EC-g-PNIPAM are shown in figure 2. Strong absorption peak at 1646-1647cm-1 indicates the presence of C=O groups in secondary amides of PNIPAM chains. Peaks at 1546-1547cm-1 and 3296-3297cm-1 are resulted from -NH groups in secondary amides of PNIPAM.

Figure 1. Effects of varying the conc.                 Figure 2. FTIR spectra of EC and ECGPN4

of NIPAM on grafting yield%

Preparation and characterization of microparticles

Figure 3 shows the SEM photograph of EC microparticles prepared by the spray drying method. SEM photograph shows that EC microparticles are spherical with a rugged surface. Figure 4 shows the SEM photograph of EC-g-PNIPAM microparticles (ECGPN8 MP) prepared by the spray drying method. Some of them have spherical shape with a rugged surface which is smoother than that of EC microparticles. However, others are partially or totally collapsed as if the air has gone out of the microparticles.

Figure 3. SEM of EC microparticles                  Figure 4. SEM of ECGPN8 microparticles

As shown in figure 5, the particle size distribution of EC microparticles is narrow with effective particle size 8.85μm. The particle size distribution of ECGPN8 microparticles are shown in figure 6. Alike EC microparticles, ECGPN8 microparticles have narrow particle size distribution and their effective particle size was 7.81μm.

Fig 5. Particle size distribution of EC MP     Fig 6. Particle size distribution of ECGPN8 MP

Drug release from microparticles

Figure 7 shows the allopurinol release from EC microparticles. The drug release at 40℃ is higher than that of 25℃. It is thought that as the temperature increases the diffusion coefficient increases, therefore the drug release at 40℃ is higher. Figure 8 shows the allopurinol release from ECGPN8 microparticles. As expected by the action of thermo-sensitive polymer, the release rate of allopurinol is lower at 40℃. It was also found that a relatively large burst effect occurred at the start of release with about 50% of drug released within the first 2h. This large burst effect may be attributed to the disadvantage of the spray drying method; the free drugs which results from the rapid solvent evaporation in the spray chamber of a spray dryer.

Figure 7. Release of allopurinol from                  Figure 8. Release of allopurinol from

ECMP at 25℃ and 40℃                                 ECGPN8MP at 25℃ and 40℃

When the temperature is increased above the LCST, the hydrophilic PNIPAM becomes hydrophobic and collapse to change into a compact form from the expanded one. Since a palisade-like hydrophobic PNIPAM blocks the release of a drug, the drug release at 40℃(above the LCST) is smaller than that of 25℃(below the LCST).

REFERENCES

1. Hiromi Kitano, Changhong Yan, Katsunori Nakamura, Makromol. Chem., 192, 2915-2923(1991).

2. Chong-Su Cho, Jae-Bok Cheon, Young-Il Jeong, Macromol. Rapid Commun., 18, 361-369(1997).

3. E.A. Abdel-Razik, Carbohydrate Polymers, 31, 23-27(1996).

4. T. Kristmundsdottir, O.S. Gudmundsson, and K. Ingvarsdottir, International Journal of Pharmaceutics, 137, 159-165(1996).

5. U. Conte, B. Conti, P. Giunchedi, L. Maggi, Drug Development and Industrial Pharmacy, 20(3), 235-258(1994).