- 고온에서 개질화된 제올라이트를 이용한 메칠아이오다이드의 흡착

- 최병선1, 박근일1 , 김준형1 , 이재욱2, 유승곤3

- 1한국원자력연구소

- 2서남대학교 환경화학공학부

- 3충남대학교 화학공학과

##### Adsoption of Methyl Iodide in a Modified Zeolite Column at High Temperatures

- Byung Seon Choi, Geun Il Park, Joon Hyung Kim, Jae Wook Lee, and Seung Kon Ryu

Korea Atomic Energy Research Institute

Faculty of Environmental & Chemical Engineering, Seonam University

Dept. of Chemical Engineering, Chungnam National University

- Introduction

Among adioactive wastes, radioiodines such as elemental iodines (I, I2), organic iodide (CH3I) and hypoiodous acid (HOI) are the most important nuclides due to their volatility and the significant radiological effects on the human body and the environment (Wren et al., 1999). The removal of radioiodines has generally been performed using activated carbon, silica, alumina, and polymer resin. Also, impregnants such as KI, TEDA (triethylene diamine), and silver have been widely used to improve the removal efficiency. Although activated carbon has been successfully used in nuclear power plants, it cannot be considered as a primary adsorbents in a high temperature system, because of its low ignition temperature and its adverse reaction with nitrogen oxide. Therefore, activated carbon is virtually ruled out for high temperature systems like the DUPIC (Direct Use of Spent PWR Fuel In CANDU Reactor) process. As a result, the promising approach to the problem of iodine removal under high temperature conditions is to use inorganic adsorbents in which a stable iodine compound is formed.

The objectives of this work are to evaluate the adsorption and dynamic characteristics of gaseous methyl iodide on silver ion-exchanged zeolites at high temperatures up to 400oC. From the standpoint of silver utilization for the removal of methyl iodide, both the optimal operating temperature and the effective silver ion-exchanged level were determined. The reliability of an adsorption process model largely depends on the adequacy of its constituent models, which represent the equilibrium isotherm, mass transfer, and heat transfer dynamics (Rutheven, 1984; Yang, 1987). In this study, a simple nonisothermal and axially dispersed plug-flow model is adopted to simulate the experimental breakthrough curves. The Langmuir-Freundlich isotherm model is used to represent the equilibrium relationship, and the linear driving force (LDF) approximation is used to represent the particle uptake.

- Theory & Model

### Governing Equations for Mobile and Stationary Phases - The following dimensionless mathematical model takes into account the combined effects of axial dispersion, film mass-transfer resistance, intraparticle diffusion, and nonisothermal adsorption isotherm.

∂X∂τ=1Pem∂2X∂χ2−2θ∂X∂χ∂θ∂χ−V∂X∂χ+ϕ(X−1)∂Y∂τ			(1)

∂V∂χ=1Pem2θ2∂θ∂χ2−1θ∂2θ∂χ2+1θ∂θ∂τ+Vθ∂θ∂χ−ϕ∂Y∂τ		(2)

∂θ∂τ=1Peh+φPem∂2θ∂χ2−φV∂θ∂χ−2φPem1θ∂θ∂χ2+φϕ(θ+ζ)∂Y∂τ	(3)

∂Y∂τ=α(Y−Y)							(4)

Y=βXn1+βXn							(5)

where, β=boexp(−ΔHA)RTf1θPfn				(6)

### Numerical Solution – The PDEs are discretized with the orthogonal collocation on finite element method, respectively. Then, these equations are converted to a first order ordinary differential equations. The ODE system is then solved with the LSODI subroutine from IMSL, which uses Gear’s stiff method for initial value ODE problems (Villadesen and Michelson, 1978; Lee et al, 1999).

## EXPERIMENTAL

The sodium form zeolite(NaX) of 8~16 mesh Linde Molecular Sieves 13X (Supplied by Aldrich Co., USA) was used as a base adsorbent to prepare silver ion-exchanged zeolite, namely AgX. AgX was prepared through the ion exchange method in a batch reactor. Zeolite was purged with water-saturated air stream at room temperature for three days to equilibrate it with moisture, which prevents bead fissure of the 13X from soaking in water. After these treatments, the zeolite was washed with distilled water to remove fines. The 13X zeolite was then immersed into the silver nitrite (AgNO3) solution of 1.2 N for 8 hours at room temperature, and washed with distilled water to remove the excess salt ions. The AgX was dried to obtain a constant weight in a vacuum oven at 180oC for 24 hours. Gaseous methyl iodide is produced from an evaporation of aqueous methyl iodide. The gas-phase concentration is adjusted by controlling the solution temperature and the nitrogen flow rate to methyl iodide generators. The effluent concentration of methyl iodide from the column was analyzed by the gas chromatography with a pulse discharged detector (PDD) and GS-Q capillary column at an oven temperature of 140oC. Both the breakthrough curve of methyl iodide adsorption and the weight change of the adsorbent were used to obtain the adsorption amount of the adsorbate. Also, desorption after adsorption of methyl iodide was conducted by controlling the column temperature.

## RESULT& DISCUSSIONS

In order to investigate the influence of silver-ion loading and temperature on the removal of methyl iodide, the adsorption of methyl iodide on the three kinds of AgX (10, 20, 30 wt%) were evaluated at four different temperatures (100, 175, 235, 400 oC). The adsorption capacity decreases with increasing temperature and with the decreasing silver ion-exchanged amount. Since a higher silver ion-exchanged level contributes to an increase of the number of Ag+ ions, the chemical reaction between Ag+ and CH3I increased on silver ion-exchanged active sites. In general, a reduction of the micropore volume and partial blocking of the active site can be observed with increasing silver ion-exchanged amounts. As listed in Table 1, however, the variation of the physical properties is small. The kinetic diameters of elemental iodine and methyl iodide are about 5 Å and 6 Å, respectively. The average pore diameters of base 13X and AgX are almost equal, approximately, 24Å. Therefore, no partial blocking may happen in the portion of unreacted silver

Table 1. Physical Properties of Silver-exchanged Zeolite

|  | MS-13X (0 wt%) | AgX (10 wt%) | AgX (20 wt%) | AgX (30 wt%) |
| --- | --- | --- | --- | --- |
| Average pore diameter, Å | 24.5 | 24.4 | 23.4 | 23.6 |
| Surface area, m2/kg | 7.99105 | 7.95105 | 7.20105 | 6.99105 |
| Total pore volume, m3/kg | 3.5610-4 | 3.2210-4 | 2.8810-4 | 2.8110-4 |
| Micropore volume, m3/kg | 2.3710-4 | 2.0510-4 | 1.92 0-4 | 1.8310-4 |

Representative experimental data for the adsorption of methyl iodide on 10wt% AgX at four different temperatures, along with their isotherm model fits, are shown in Fig 1. The nonlinearity of the isotherm in terms of temperature was almost similar, but the saturation amount is quite different. As listed in Table 2, the isotherm parameters were extracted simultaneously from all the sets of equilibrium data obtained at different temperatures using multivariable, nonlinear regression. In this regard, a modified Levenverg-Marquardt algorithm was used (IMSL routine DUNLSF).

Table 2. Nonisothermal Model Parameters of Methyl Iodide on Silver-Exchanged Zeolites (AgX 10wt%)

| Model | Langmuir |  |  | Langmuir-Freundlich |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Parameters | qm | b0 | −ΔHA | qm | b0 | −ΔHA | n |
| Values | 1.432 | 0.369 | 2.369x104 | 2.203 | 0.344 | 7.286x103 | 5.156 |

Figs. 2 show the experimental breakthrough curves in a deep bed length at L=10cm to compare the influence of thermal effect. The solid lines represent the simulated result based on isothermal and nonisothermal adsorption equilibrium model. From this result, the heat effect due to an exothermic reaction in the deep bed should be accounted for in the model prediction, compared to one in a shallow bed. However, the magnitude of heat effect is not seem to be high as shown in Fig. 2 with temperature profiles. In especial, the breakthrough curve for the longer bed at 400 oC showed abnormal behavior. This result has not been reported so far. In our laboratory, some efforts have been focused to reveal the reaction mechanism for this result. Although no precise reaction mechanism could be proposed from the experimental data obtained so far, the following mechanism can be assumed :

2CH3I+2Ag←→2AgI+C2H6  or	2CH3I+2Ag+12O2←→2AgI+CH3OCH3

## References

Lee, J.W. and H. Moon, “Effect of pH on Adsorption of Cephalosporin C by a Nonionic Polymeric Sorbent”, Adsorption, 5, 381-390(1999).

Ruthven, D.M., Principles of Adsorption and Adsorption Process. Wiley, New York (1984)

Villadsen, J., and M.L. Michelsen, Solution of Differential Equation Methods by Polynomial Approximation, Prentice-Hall, Engleweed Cliffs, (1978).

Wren, J.C., C.J. Moore, and M.T. Rasmussen, “Methyl Iodide Trapping Efficiency of Aged Charcoal Samples from Bruce-A Emergency Filtered Air Discharge Systems,” Nuclear Technology, 125, 28-39 (1999).

Yang. R. T., Gas Separation by Adsorption Processes, Butterworths Boston(1987)

Fig. 1. Adsorption isotherm of methyl idodide on 10wt% AgX in terms of temperature.

Fig. 2. Experimental and simulated breakthrough curves of methyl idodide.