- 비이온성 고분자 흡착제를 이용한 클로로 페놀류의 흡착

- 고주영, 주성균, 심왕근, 이재욱*, 문 희

- 전남대학교 응용화학부

*서남대학교 화학공학과

- Adsorption for Chlorinated Phenols on Nonionic Polymeric Sorbent

- Ju Young Ko, Seong Kyun Ju, Wang Geun Shim, *Jae Wook Lee, Hee Moon

Faculty of Applied Chemistry, Chonnam National University, Kwangju 500-757

*Department of Chemical Engineering, Seonam University, Namwon 590-170

- Introduction

Because of their widespread use in industry, such as the pulp and paper industry, and their toxicity and recalcitrance, chlorophenolic compounds constitute an important class of environmental pollutants. Chlorophenols have found use as pesticides biocides, and monochlorophenols can be formed during the breakdown of pesticides and other chlorinated aromatic compounds. Furthermore, some of the less chlorinated chlorophenols (especially monochlorophenols) can be generated during the chlorination of wastewaters (Pritchard et al., 1987). Because of their relatively high solubility, chlorophenols cannot only contaminate wastewaters and groundwaters but also migrate within different aqueous environments (Smith and Novak, 1987).

Adsorption has been considered to be the ‘best available technology’ for removing organics from water in the US Safe Drinking Water Act (1986), (Ram, et al., 1990). The efficiency of the process is, however, dependent on the type of pollutant present and type of adsorbent chosen.

In this work, the equilibrium amounts and kinetic data for chlorophenols such as 2-chlorophenol and 2,4-chlorophenol on nonionic polymeric sorbents are measured.

- Theoretical

- Among well-known adsorption isotherms for single species, the Langmuir equation was used to fit experimental equilibrium data. The Langmuir equation represented by

- q=qmbC1+bC

- where qm is the amount of adsorption and b is empirical constant of the Langmuir equation.

##### Surface Diffusion Model

In the surface diffusion model, adsorption of adsorbates occurs at the outer surface of the particle, followed by diffusion of adsorbate molecules in the adsorbed state along the pore walls inside the particle. The driving force is the concentration gradient of the adsorbed adsorbate on the pore walls. A material balance for spherical particle results in the following mass transfer equations:

- ∂q∂t=1r2∂∂r(r2Ds∂q∂r)

kf(C−Cs)=Dsρp∂q∂r     at   r = Rp

∂q∂r=0    at r = 0

##### Pore Diffusion Model

In the pore diffusion model, diffusion of molecules occurs in the pore fluid and adsorption takes place when molecules reach the adsorption sites. Based on the assumption of a spherical particle, dilute solution, and local equilibrium, the adsorbate mass transfer equations are as follows:

εp∂Cp∂t+ρp∂q∂t=εpr2∂∂r(r2Dp∂Cp∂r)

kf(C−Cs)=εpDp∂Cp∂r    at   r = Rp

∂Cp∂r=0     at   r = 0

- Experimental Section

The adsorbents used in this study were XAD-7. Amberlite XAD-7 is a macroreticular and spherical polystyrene resin cross-linked with acrylic ester polymer which was supplied by Rohm and Haas Co. (Spring House, PA). Its physical properties are listed in Table 1.

The adsorbates used in this study were 2-chlorophenol (2-CP), 2,4-dichlorophenol (2,4-DCP) and for a comparison Phenol (Ph) were used. They are purchased from Aldrich Chemical Co. (Milwaukee, WI). Their solubility and molecular weight are listed in Table 2.

Adsorption amounts were obtained by a batch method. Preweighed amounts of hydrated XAD-7 were placed in test tubes containing 20ml of a solution with a known initial solute concentration. The tubes were then placed on a shaker for a period of 7 days in a temperature-controlled oven. After equilibrium, a UV spectrophotometer (Varian, model DMS 100s) was used to measure the adsorbate concentration in the solution. Wavelengths of 270, 270.6 and 281.1nm were used for Ph, 2-CP and 2,4-DCP, respectively. The equilibrium amount of solute adsorbed was then calculated by a mass balance.

Adsorption experiments were conducted in a Carberry type batch adsorber shown in Fig. 1. The pretreated resin particles were put inside the cage affixed to the shaft wings. The cage containing polymeric resin was put immediately into distilled and deionized water to saturate the pores within the particles with water. At a given starting time, the cage was lifted from the container with water and put into the vessel. Experiments were carried out at 500 rpm. Liquid samples were taken periodically by using an airtight precision syringe, withdrawing the solution from the vessel through the sample hole.

Table 1. Properties of Sorbents

| Adsorbent | # Unit | XAD-7 |
| --- | --- | --- |
| Chemical structure | - | Acrylic |
| Particle size | ㎛ | 430-690 |
| Particle porosity | - | 0.57 |
| Moisture content | % | 67 |
| Surface area ( BET ) | m2/g | 450 |
| Average pore diameter | oA | 90 |

Table 2. Properties of ph, 2-CP and 2,4-DCP at 25 ℃.

| compound | solubility in water(g/100 mL) | molecular weight |
| --- | --- | --- |
| phenol | 8.15 | 94.113 |
| 2-chlorophenol | 2.85 | 128.56 |
| 2,4-dichlorophenol | 0.45 | 163.00 |

- Results and Discussion

As illustrated in Fig. 2 adsorption amount of 2,4-DCP on XAD-7 is greater than that of Ph and 2-CP. The experiment data are well correlated by Langmuir equation. The Langmuir parameters, qmand b, were fitted to the data by a nonlinear least-squares fitting routine(MINPACK in the IMSL package) and listed in Table 3.

Table 3. Langmuir Parameters for the Adsorption of Ph, 2-CP and 2,4-DCP 
on XAD-7 at 25℃.

| compound |  | Ph | 2-CP | 2,4-DCP |
| --- | --- | --- | --- | --- |
| #### XAD-7 | qm | 0.655 | 0.626 | 0.111 |
|  | b | 0.587 | 0.330 | 0.724 |
|  | E(%) | 6.209 | 8.107 | 13.593 |

Error(%)=100Nk=1Nqexp,k−qcal,kqexp,k

The estimated values of kf and Ds obtained from batch experimental data are listed in Table 4. The effective diffusion coefficient estimated by this method reflects all kinds of mass transfer resistances inside a particle. The surface diffusion coefficients obtained are in the range 0.50 ~ 0.26  10-11 m2/s for Chlorophenols used here.

Figs. 3 ~ 4 represent the experimental and simulated data for Chlorophenols in a batch adsorber. The adsorption model shows satisfactory prediction of concentration decay curves using kf and Ds.

Table 4. Kinetic parameters in a batch reactor

| compound | kf × 105 m/sec | Ds × 1011 m2/sec | Dp × 109 m2/sec |
| --- | --- | --- | --- |
| 2-CP | 2.25 | 0.50 | 4.19 |
| 2,4-DCP | 5.90 | 0.26 | 1.41 |

## References

- Colella, L. S.; Armenante, P. M.; Kafkewitz, D.; Allen, S. J.; Balasundaram, V. “Adsorption Isotherms for Chlorinated Phenols on Activated Carbons”, J. Chem. Eng. Data 1998, 43, 573-579

2.  Moon, H., Soon Ki Kook and Heung Chul Park, “Adsorption of Phenols onto a polymeric sorbent”, Korean Journal of Chemical Engineering, Vol. 8, No. 3, pp 168~176 (1991)

3

0

Motor

Opening

Cap

Water

Outlet

Baffle

Water

Inlet

ψ

90

10 mm

35

mm

135

50 mm

Fig. 2. Adsorption Isotherms for XAD-7
        showing effects of the adsorbate at 25℃

Fig. 3. Observed and predicted uptake curves of 2-CP on XAD-7.

(V=2L, W=0.99g, and C0=1mol/m3)

Fig. 1. Schematic diagram of experimental
batch reactor

Fig. 4. Observed and predicted uptake curves of 2,4-DCP on XAD-7.

(V=2L, W=0.99g, and C0=1mol/m3)