- MCM-48에서 휘발성 유기용제의 흡착열 계산

- 양문상, 심왕근, 이재욱*, 서숭혁**, 문  희

- 전남대학교 응용화학학부

- 서남대학교 화학공학과*

- 계명대학교 화학공학과**

Isosteric Heat of Adsorption of VOCs on MCM-48

- Moon Sang Yang, Wang Geun Shim, Jae Wook Lee*, Soong Hyuck Suh**, Hee Moon

Faculty of Applied Chemistry, Chonnam National University, Kwangju

Department of Chemical Engineering, Seonam University, Namwon*

Department of Chemical Engineering, Keimyung University, Dae Gu**

### Introduction

In adsorption processes, the equilibrium data obtained should be correlated by isotherm equation which can represent experimental data well. Most of isotherm equations contain two or more parameters which can be correlated with temperature, and this temperature dependency allows one to predict adsorption equilibria over broad range of temperature [1-3].

In this study, we applied two approaching method to determine isosteric heat of adsorption, that is, (i) a thermodynamic method based on the assumption that the isosteric heat of adsorption is independent of temperature, and (ii) a method to use an isotherm equation which includes the parameters as a function of temperature. The major advantage of thermodynamic method is that the adsorption equilibria at various temperatures could be estimated using experimental data at only two temperatures. In order to determine the isosteric heat of adsorption, the adsorption equilibrium experiments of VOCs (benzene, n-hexane, cyclohexane, methanol) on mesoporous materials (MCM-41 and MCM-48) were carried out at 303, 313 and 323 K. A hybrid model combined both Langmuir and Langmuir-Freundlich equations was used to correlate equilibrium data obtained at different temperatures.

- Theoretical Model

It has been generally known that the adsorption is accompanied by evolution of heat since adsorbate molecules are more stabilized on the adsorbent surface than in the bulk phase. The isosteric heat of adsorption, qst, is defined by the equation of the Clausius-Clapeyron type (1);

qst=RT2∂lnP∂TN                                                     (1)

The equation, when integrated, allows one to calculate qst from adsorption isotherms obtained experimentally at two or more temperatures, provided the range of temperatures is small enough to justify the assumption that qst is independent of temperature.

qst=RlnP1−lnP21T1−1T2N                                              (2)

where P1 and P2 are the equilibrium pressures at temperatures T1 and T2 respectively, when the amount adsorbed is N. Prediction is based on the assumption that the isosteric heat of adsorption is independent of temperature.

The equilibrium data for mesoporous sorbents are fitted to combined model of Langmuir and Langmuir-Freundlich equations. The hybrid isotherm model with four isotherm parameters is as below:

q=qmb1P1+b1P+b2Pn1+b2Pn                                             (3)

where the isotherm parameters as a function of temperature are as follows:

qm=qm0expαR1T−1Tm                                             (4)

b1=b10exp−ΔH1R1T−1Tm                                          (5)

b2=b20exp−ΔH2R1T−1Tm                                         (6)

n=n0exp−βR1T−1Tm                                             (7)

Applying Eq (3) with temperature-dependent isotherm parameters of Eqs (4)-(7) to Eq. (1) gives the derived isosteric heat of adsorption as below:

qst=b1−ΔH1+αb1+αb12P1+b2Pn2b11+b2Pn2+b2nPn−11+b1P2+b2Pn−1−ΔH2+b2nPn−1lnP−β+αb2Pn−1+αb22P2n−11+b1P2b11+b2Pn2+b2nPn−11+b1P2 	        (8)

TC

1

3

BP

Vacuum

System

Computer

2

Temperature

Controller

4

TC

TC

BP

BP

Readout

Unit

Experimental

The measurement technique to determine adsorption amount was the gravimetric method. Adsorption amounts are measured using a quartz spring beam. 0.5~0.1g of adsorbents (MCM-41, MCM-48) in quartz basket is ventilated to remove impurities within the adsorbents at 573.15K for approximately 4h by using a vacuum pump. Adsorption amounts are measured at respectively different temperature of 303, 313, and 323 K. A schematic diagram of the apparatus is shown in Figure 1. The thermostat bath surrounding the adsorbent was maintained at the required temperature within  ±0.5℃. 							    Fig. 1. Experimental apparatus.

The adsorption equilibrium was usually attained within 40-60min. The adsorbent (0.5~0.1g) was dried and degassed. The temperature was increased at a rate of 10℃/min up to 200~300℃ to remove impurities of adsorbent and held constant at this value for 4 h.

### Results and Discussion

Fig. 2 shows the adsorption isotherms of the benzene and cyclohexane at 303, 313 and 323 K. In general, the adsorption capacity was decreased with increasing temperatures. This implies that the adsorption of VOC on mesoporous sorbents is the physical adsorption. As listed in Table 1, the temperature-dependant isotherm parameters for powder and palletized MCM-48 were determined by nonlinear fitting from all isotherm data determined at different temperatures. Fig. 3 shows the dependence of the isosteric heat of adsorption for benzene on MCM-48. The isosteric heat of adsorption with loadings was calculated from Eq. (8) with parameters listed in Table 1.The isosteric heat for powder MCM-48 is approximately 43 kJ/mol between the adsorption amounts of 2.0 to 6.0 mmol/g, but that is 38 kJ/mol between the adsorption amount of below 2.0 mmol/g and above 6.0 mmol/g. This difference comes from the capillary condensation. The sharp variation of heat of adsorption for benzene with surface coverage supports that bonding among benzene molecules in the condensed phase and between adsorbed benzene layer and MCM-48 surfaces play a key role in determining the desorption characteristics because the isosteric heat of adsorption is considered as the isosteric enthalphy of desorption. MCM-48 surface seems to be heterogeneous because the isosteric heat of adsorption is changed according to the loading. It has been recognized that surface heterogeneity may come from the energetic, structural and geometric heterogeneity. The surface heterogeneity here resulted from structural heterogeneity because the capillary condensation is highly sensitive to structure properties of pore size and pore distribution.

Table 1 Hybrid Isotherm Parameters and Heat of Adsorption

|  | Powder | Pellet |
| --- | --- | --- |
| qm | 6.466 | 4.527 |
| b1 | 7.58×10-2⋅exp36595RT | 1.37×10-1⋅exp32565RT |
| b2 | 4.44×10-16⋅exp1293916RT | 2.94×10-16⋅exp723311RT |
| n | 2.04×101⋅exp12547RT | 1.92×101⋅exp102RT |
| ###### ΔH | 43 kJ/mol | 38 kJ/mol |

Reference

[1] Gregg, S.J. and K.S.W. Sing, Adsorption, Surface Area and porosity, Academic Press. (1982)

[2] X.S. Zhao et al. Colloids and Surfaces A: Physixoxhem. Eng. Aspects 179 (2001) 261-269

[3] J.H. Yun, Journal of Chemical Engineering, 46 (2001) 156-159

Fig. 2. Adsorption isotherms of benzene and cyclohexane on MCM-48.

Fig.3. Isosteric het of adsorption of benzene in MCM-48.