고분자 전해질의 상거동

고 성진, 배 영찬

Phase behaviors of solid polymer electrolyte/salt systems

- Dept. of Industrial Chemistry and Molecular Thermodynamics Lab.

- Hanyang University, Seoul 133-791, Korea

Abstract

In the conventional rechargeable lithium batteries, a nonaqueous solvent is used as an electrolyte. It is because lithium deposited upon charging is readily reactive with moisture.

Recently, much work is devoted to the development of electrolytes based PEO(polyethylene oxide) that shows good electrochemical and mechanical properties. In this study, we propose a new thermodynamic model based on the perturbed hard sphere chain (PHSC) model and the melting point depression theory to predict the phase behaviors of PEO/salt systems. PHSC model uses the modified Chiew equation of state and van der Waals perturbation whose parameters are related to the intermolecular potential. Theoretical coexistence curves are compared with experimental data for various PEO/salts systems.

# Teory

1. PHSC(Perturbed Hard Sphere Chain ) Theory

PρkT=1+ρi=1mj=1mxixjk=lril=1rjbij,klgij,kl−i=1mxik=1ri−1gii,k,k+1−1−ρkTi=1mj=1mxixjk=1ril=1rjaij,kl     The equation of state for mixtures is

Where, xi=Ni/N is the mole fraction of molecules, ri is the number of hard spheres, and gij is the pair radial distribution functioㅜ of hard-sphere mixtures at contact, which takes the form given by Boublik-Manxoori-Carnahan-Starling (BMCS) equation:

gij,kl=11−η+32ξij1−η2+12ξij21−η3

η=ρ4i=1mxiribiWhere  η and ξij are given by

ξij,kl=ρ4bibjbij13k=1mxkrkbk23

  - Thermodynamic functions

The general equation for calculating the Helmholtz energy from the equation of state is:

A(T,V,Ni)=imAi0(T)+P−NkBTVdV+kBTimNilnNkBTV

Equation can be written in terms of T, ρr, and φi :

ANrkBT=imϕiriAioNikBT+ρri,j=1mφiφjbijWij−i=1mφi1−1riQii

−ρrkBTi,j=1mφiφjaij+i=1mφirilnφiriρrkBT                   (1)

where

Wij=1ρrgijdρr=I1η+32ξijη2I2+12ξij2η3I3

Qij=Qij(η,ξij)=(gij−1)dρrρr=−ln(1−η)+32ξij1−η+14ξij2(1−η)2

with

In=−In−1+1n−1ηn−1(1−η)n−1 ,   I1=−ln(1−η)

The chemical potential can be found by differentiation of eq.(1)

μk=∂A∂NkT,V,Ni≠k

The result is

μkkBT=μ0kBT+2rkρri=1mφibikWik+ρri,j=1mφiφjbij×Nr∂Wij∂Nk

−rk−1Qkk−i=1mφi1−1ri×Nr∂Qii∂Nk−2rkρrkBTi=1mφiaik+lnφkrkρrkBT+1     (2)

2. The melting point depression theory

In a semicrystalline system, the condition of equilibrium between a crystalline polymer and the polymer unit in the solution may be described as follows

μuc−μu0=μu−μu0                              (3)

where μuc, μu, and μu0 are chemical potentials of crystalline polymer segment unit, liquid (amorphous) polymer segment unit and chemical potential in standard state, respectively. Now the formal difference of appearing on the left-handed side is expected as follows :

μuc−μu0=−ΔHu(1−T/Tm0)                          (4)

where ΔHu is the heat of fusion per segment unit, T and Tm0 are melting point temperature of the species in a mixture and the pure phases, respectively. The right-handed of eq.(3) can be restated from eq.(2).

## Conclusion

(PEO/LiCF3SO3  system)                   (PEO/ZnCl2 system)

Figures shows phase behaviors of PEO/ salts system. Dark circles and open circles are measured by TOA and solid lines are calculated from the proposed model. From the proposed model which describes thermodynamic equilibrium of the amorphous phase with the crystalline phase is used for the calculation of the salt rich curve. The density of PEO and salt are calculated by the equation of state and the fusion enthalpy of PEO and salt are measured by DSC.

As shown in figures, the theoretical prediction not only gives fairly well an agreement with experimental results but also identifies the eutectic point at the intersection of the two liquidus curves.