고분자 용액의 용매의 활동도: 그룹 기여 방법

장 봉호, 배 영찬

한양대학교 공업화학과 분자열역학연구실

Solvent Activity of Polymer Solution: Group-contribution Method

Bong Ho Chang, Young Chan Bae

Dept. of Industrial Chemistry and Molecular Thermodynamics Lab.

Hanyang University, Seoul 133-791, Korea

Abstract

A specified group-contribution method is proposed to estimate vapor-liquid equilibria (VLE) of ordinary and associated binary polymer solutions. In this group contribution method, the van der Waals (vdW) energy parameters for dispersion and polar forces and the hydrogen bonding (h-b) energy parameters for associated systems are tabulated separately. For specificity, two cases are respectively taken into accounts for associated systems. The one contains that the interactions between segments of polymer and solvents are similar to those between solvent segments. The other is the case having the differences between them. For the latter case, the temperature dependence of h-b parameter is introduced. Our proposed model shows good agreements with experiments in solvent activity estimations for ordinary and associated binary polymer solution.

Theory

The solvent activity is

lna1=ΔmixμNrkT=lnφ1+1−r1r2φ2+z2q1lnθ1φ1+θ1−φ2q1+r1φ2r2φ1φ1−θ1q2 +r1φ22I+r1φ22φ1∂I∂φ1I=12φ1φ2C1T−Ba1(2φ2−1)ln1−a1(2φ2−1)1−a0(2φ2−1)exp(1/T)−1

a0=0.00012+0.22999(r2−1)1+1.37129(r2−1)

a1=−0.01717+0.02160(r2−1)1+0.09642(r2−1)

b0=5.79880−1.45604(r2−1)1+1.83417(r2−1)

b1=−1.42112−0.16059(r2−1)1−1.34296(r2−1)

A dimensionless temperature is defined by T=kTε, where k is a Boltzmann's constant. ri, φi and

θi are the number of segments per molecule, volume fraction, and surface fraction of component i, respectively. The determining procedures for Equations are described elsewhere[1].

If h-b interaction occurs between the segments of molecules, following the definition of ε, we replace ε by

ε/kT−ΔAsec,ii/NiikT−ΔAsec,jj/NjjkT+2ΔAsec,ij/NijkT

to incorporate a secondary lattice. Their expression is given by

ΔAsec,ijNijkT=2zηlnη+1−ηln1−η+zCαδεij1−ηη1+Cαδεij1−ηη

<Group-contribution method>

vdW energy contribution

For a pure component, vdW energy (dispersion and polar forces), εiik, can be estimated by

εiik=δd2+δp2⋅Vmi(298.15K)3⋅R⋅ri

where R is universal gas constant, and where δd, δp and Vmi(298.15K) are Hansen’s solubility parameters of a dispersion and a polar contribution and a molar volume of component i at 298.15K, respectively. The chain

length, ri, is calculated by

ri=Vmi(vdW)10.23cm3mol

where the constant 10.23cm3/mol is the molar vdW volume of a CH2 group from Bondi and Vmi(vdW) is the molar vdW volume of component i.

The vdW energy parameter, εijk, is calculated from pair-interaction group parameters

εijk=m=1Nsn=1NpφmφngmnvdW

where Ns and Np are number of groups in solvents and polymers, and where φm and φn are volume fractions of group m in a solvent and that of group n in a polymer, respectively (Case I). gmnvdW is vdW pair interaction parameter between group m in a solvent and group n in a polymer. For accuracy, a functional group in a polymer and that in a solvent are regarded as distinguishable.

H-b energy contribution

Hansen’s h-b solubility parameter, δh, is related to the molar additional specific energy, ΔUsec,iim, of component i by

ΔUsec,iim=−δh2⋅Vmi(298.15K)

To obtain δεiik, on inserting Equation (16) into a fundamental relation,

∂ΔAsec,iiNiikT∂1T=ΔUsec,iiNiik

we have

ΔUsec,iim=zriRTCαδεij1−ηη1+Cαδεij1−ηη2

For the Case II, cross h-b energy parameter is calculated from pair h-b interaction group parameter.

δεijk=m=1Nsn=1Npφmφngmnh−b

For the Case III,

δεijk=m=1Nsn=1Npφmφn(gmnh−b,H−T⋅gmnh−b,H)

where gmnh−b,H and gmnh−b,Sare enthalpic and entropic pair h-b interaction parameters, respectively.

Conclusion

Solvent activities for PEO (Mw=1460)/water at 297.75K(a), 307.75K(b).

Nevertheless we introduce several assumptions for simplicities, our proposed group-contribution method describes remarkably well VLE for ordinary (Case I) and associated (Case II and III) polymer solution. H-b pair interaction parameters by the secondary lattice concept are very important role in the associated polymer systems. In addition, for the aqueous polymer solution, the temperature dependent pair interaction parameters are needed to give the better agreement with experimental results.

References

[1] A. Fredenslund, R. L. Jones, J. M. Prausnitz, AlChE J. 1977, 21, 1086.

[2] T. Oishi, J. M. Prausnitz, Ind. Eng. Chem. Proc. Des. Dev. 1978, 17, 333.

[3] E. C. Voutsas, D. P. Tassios, Ind. Eng. Chem. Res. 1996, 35, 1439.

[4] C. Mollamann, J. Gmehling, J. Chem. Eng. Data 1997, 42, 35.

[5] S. Zhang, T. Hiaki, M. Hongo, K, Kojima, Fluid Phase Equilibria 1998, 144, 97.

[6] T. Magnussen, P. Rasmussen, A. Fredenslund, Ind. Eng. Res. 1981, 20, 331.

[7] P. A. Gupta, R. P. Danner, Ind. Eng. Chem. Res. 1987, 26, 2036.

[8] H. H. Hopper, S. Michel, J. M. Prausnitz, Ind. Eng. Chem. Res. 1988, 27, 2182.

[9] T. Holderbaum, J. Gmehling, Fluid Phase Equilibria 1991, 70, 251.

[10] M. S. High, R. P. Danner, Fluid Phase Equilibria 1990, 55, 1.

[11] E. A. Guggenheim, Mixtures. Clarendon Press, Oxford, Chaps. 4. 10. and 11.

[12] S. M. Lambert, D. S. Soane, J. M. Prausnitz, Fluid Phase Equilibria 1993, 83, 59.

[13] B. H. Chang, Y. C. Bae, Polymer 1998, 39, 1735.

[14] K. F. Freed, J. Phys. A: Math. Gen. 1985, 18, 871.

[15] J. S. Oh, Y. C. Bae, Polymer 1998, 39, 1149.

[16] D. W. van Krevelen, “Properties of Polymers”, 3rd edn. Elsevier, Amsterdam, 1990.

[17] H. Wen, H. S. Elbro, P. Alessi, “Polymer Solution Data Collection, Part I: Vapor-

Liquid Equilibrium”, DECHEMA, Frankfurt, 1992.